Optimizing Endothelial Cell Adhesion and Invasion with Naturally-Derived, Biodegradable Hybrid Hydrogel Scaffolds

Alyssa J. Reiffel, MD; Justin L. Perez, BS; Allie M. Sohn, MD; Edo Israely, BA; Natalia Jimenez, BS; Jason A. Spector, MD

Abstract

Background:  Cellular ingrowth and neovascularization of acellular scaffolds represent the rate-limiting steps of tissue-regeneration matrix incorporation.  In an effort to determine the material specifications that allow for maximal cellular invasion, we evaluated human umbilical vein endothelial cell (HUVEC) adherence and invasion into naturally-derived, biodegradable hybrid hydrogel scaffolds in an in vitro wound healing model.

Methods:  Hydrogel scaffolds were fabricated to consist of the following compositions: alginate, alginate+collagen type I in 5:1 and 10:1 (w/w) ratios, alginage+chitosan in 1:1 and 2:1 ratios, and alginate+collagen+chitosan in a 10:2:5 ratio.  All scaffolds were Arg-Gly-Asp (RGD)-modified.  Additional alginate+collagen 10:1 scaffolds were fabricated to contain an internal biodegradable polyglactone mesh to allow for suture fixation to a recipient site.  Scaffolds were seeded with 3.0x105 HUVECs, maintained under standard cell culture conditions for 14 days, and fluorescently labeled with DiI-Ac-LDL.  Cell density and invasion into scaffolds were evaluated using 3-dimensional confocal imaging.

Results:  HUVECs were maximally confluent on alginate+collagen (5:1 and 10:1) hybrid scaffolds compared with pure alginate scaffolds (163.6±27.6 and 221±19.8 v. 5.9±0.9 cells/HPF, p<0.001).  Cellular adhesion to alginate+chitosan 1:1 scaffolds was greater than to pure alginate scaffolds (9.8±1.4 v. 5.9±0.9, p=0.02) but less than collagen-containing scaffolds (p<1.0x10-5). Cellular adhesion to alginate+chitosan 2:1 scaffolds was greater than to pure alginate scaffolds (151.6±21.4 v. 5.9±0.9, p<1.0x10-7), unchanged from alginate+collagen 5:1 scaffolds, and less than to alginate+collagen 10:1 scaffolds (p=0.02).  Three-dimensional imaging revealed that cells traversed the greatest distance through collagen-containing hydrogels.  HUVEC adhesion alginate+collagen 10:1 hybrid scaffolds was not decreased by the presence of mesh.

Conclusions: Even at low concentrations, the addition of collagen type I to alginate matrices results in a substantial increase in HUVEC adherence and invasion.   These findings provide important insights into the optimization of endothelial cell adhesion and invasion by appropriate substrate selection.

Disclosure/Financial Support

A portion of this research was funded by a Ruth L. Kirschstein National Research Service Award (Kirschstein-NRSA) Institutional Research Training Grant (T32 HL083824 05 to Dr. Alyssa J. Reiffel) and the Weill Cornell Medical College Clinical and Translational Science Center (TL1RR024998 to Natalia Jimenez).

None of the authors have any commercial associations or financial disclosures that might pose or create a conflict of interest with information presented in this manuscript.