High-Fidelity Tissue Engineering of Patient Specific Auricles for Reconstruction of Pediatric Microtia

Alyssa J. Reiffel, MD; Bryan N. Brown, PhD; Karina A. Hernandez, DO; Sherry Zhou, MEng; Lawrence J. Bonassar, PhD; Jason A. Spector, MD

Abstract

Background: We sought to combine digital photogrammetry with computer-assisted design/computer-assisted manufacturing (CAD/CAM) techniques to develop biocompatible tissue-engineered auricular reconstructions that would more closely mimic the normal anatomy of the patient-specific external ear and the complex mechanical behavior of native elastic cartilage, while avoiding the morbidity and poor aesthetic outcomes typically associated with traditional reconstructions.1-5

Methods: The three-dimensional structures of normal pediatric ears were digitized using the Cyberware® 3D Digitizer.  Images were converted to virtual solids using Geomagic Studio® and translated into volume models for mold design.  Image-based synthetic reconstructions of these ears were fabricated under sterile conditions from collagen type I hydrogels cast from these three-dimensional molds. One group of constructs was seeded with 2.5x10^7 bovine auricular chondrocytes. Cellular and acellular constructs were implanted subcutaneously in nude rats and harvested after 4weeks.

Results: Post-implantation, cellular constructs effectively maintained the anatomical features of the external ear including tragus, lobule, helix, and antihelix.  Post-harvest weight of cellular specimens was significantly greater than that of acellular specimens (4.2±0.29g v. 0.80±0.12g, p=<0.05). Safranin O-staining revealed that only cellular constructs demonstrated evidence of a self-assembled perichondrial layer and cartilage deposition by lacunar chondrocytes (Figures 1-2).  Verhoeff staining of cellular constructs revealed elastin fibers interspersed among the chondrocytes.  The confined compression modulus of cellular constructs increased significantly from 9.2±1.4kPa pre-implantation to 31±14kPa at 4weeks (p<0.05).

Conclusions: We have successfully combined digital photogrammetry with CAD/CAM techniques to create biocompatible patient-specific human-sized tissue-engineered constructs for ear reconstruction. The cellular constructs’ life-like biomechanical properties and maintenance of volume, shape and topographical characteristics over time can be attributed in part to their unique type I collagen composition.  Furthermore, this material chemistry allows for chondrocyte survival and the in vivo deposition of elastic cartilage. We believe our approach to auricular tissue engineering holds tremendous promise for translation to the clinical realm.

References

1.	Shieh, S.J., Terada, S., Vacanti, J.P. Tissue engineering auricular reconstruction: in vitro and in vivo 	studies. Biomaterials 25: 1545-1557, 2004.

2.	Bichara, D.A., O'Sullivan, N.A., Pomerantseva, I., et al. The tissue-engineered auricle: past, present, and 	future. Tissue Eng Part B Rev 18: 51-61, 2012.

3.	Haisch, A., Klaring, S., Groger, A., et al. A tissue-engineering model for the manufacture of auricular-	shaped 	cartilage implants. Eur Arch Otorhinolaryngol 259: 316-321, 2002.

4.	Rodriguez, A., Cao, Y.L., Ibarra, C., et al. Characteristics of cartilage engineered from human pediatric 	auricular cartilage. Plast Reconstr Surg 103: 1111-1119, 1999.

5.	Liu, Y., Zhang, L., Zhou, G., et al. In vitro engineering of human ear-shaped cartilage assisted with 	CAD/CAM technology. Biomaterials 31: 2176-2183, 2010.

Disclosure/Financial Support

This work was supported in part by the Ruth L. Kirschstein National Research Service Award (T32 HL083824-05) Institutional Research Training Grant (Dr. Reiffel).

None of the authors has a financial interest in any of the products, devices, or drugs mentioned in this manuscript.