Optimal Murine Cranial Defect Reconstruction Utilizing a Novel Collagen Scaffold and rhBMP2 with Analysis Utilizing Confocal Microscopy

Christopher Madsen MD, Denver Lough MD PhD, Qiongyu Guo PhD, Edward Swanson MD, Nikolai Sopko MD PhD, Devin Miller BS, Gerald Brandacher MD, Anand Kumar MD

The Johns Hopkins Hospital, Department of Plastic & Reconstructive Surgery

Introduction

Although tremendous advancements in the surgical reconstruction of craniofacial defects have been made, a large proportion of patient outcomes remain unfavorable. Patients with combat and civilian trauma, craniectomy for various intracranial pathologies and large en-bloc tumor resections are often left with few reconstructive options.  Technical challenges that exist in the reconstruction of larger, more complex craniofacial defects are pronounced due to a higher incidence of infection, soft tissue erosion, extrusion, and migration. This study aims to further delineate the role of bone morphogenetic protein-2 (rhBMP2) by determining the smallest dose required for maximal bone regeneration when delivered in a novel collagen scaffold.

Methods

Utilizing a murine model, C57BL/6 (n=) mice received two identical 5mm full-thickness craniectomy defects (61.6 mm2) using a standardized micro-drill core bit. The mice were divided into 10 groups consisting of: craniectomy only (Group 1, n=3), craniectomy with doses of 0.1µg rhBMP2 (Group 2, n=3), 1.0µg rhBMP2 (Group 3, n=3), 2.5µg rhBMP2 (Group 4, n=3), 5.0µg rhBMP2 (Group 5, n=3), craniectomy with collagen only (Group 6, n=3), and craniectomy, collagen and doses of 0.1µg rhBMP2 (Group 7, n=5), 1.0µg rhBMP2 (Group 8, n=5), 2.5µg rhBMP2 (Group 9, n=5), 5.0µg rhBMP2 (Group 10, n=5). Mice underwent CT imaging at 2 and 8 weeks to assess volumetric calvarial bone regeneration and explant analysis at 8 weeks using confocal microscopy.

Results

The mice in Group 1 (craniectomy only), Groups 2-5 (craniectomy plus rhBMP2) and Group 6 (craniectomy plus collagen) showed appreciable but little total percent defect healing at 8 weeks (Group 1=1%, Group 2=9%, Group 3=12%, Group 4=13%, Group 5=19%, and Group 6=4%). Groups 7-10 (craniectomy plus collagen plus rhBMP2) showed a much higher stepwise increase in total percent of defect healed (Group 7=19%, Group 8=23%, Group 9=31%, and Group 10=38%).  Additionally, a stepwise increase in total hydroxyapatite aggregates and hydroxyapatite aggregate size was observed in Groups 2-5, and Groups 6-10. Maximum angiogenesis was seen in Group 8.

Conclusions

Current surgical reconstruction of large craniofacial defects remains challenging and associated with a high incidence of complications.  The determination of an optimal dose of rhBMP2 delivered in a novel collagen scaffold, as outlined here in a murine cranial defect, facilitates further evaluation of rhBMP2 when used alone or in combination with other biologic products to reconstruct large craniofacial defects.